High Drain Rechargeable Battery Datasheet

Of

KeepPower IMR26650 4200mAh

# 1. Specification

| 1.1 | Rated Charge(1C) | 3.5A CC charge to 4.2V, then 4.2V CV charge until current less than 50mA at 23±2°C. |
| --- | --- | --- |
| 1.2 | Recommended charge | Reference 1A |
| 1.3 | Rated discharge(0.2C) | Constant 0.7 A discharge until 2.5V at 23±2°C. |
| 1.4 | Discharge cut-off voltage | 2.5V (End of discharge voltage after recommended charge). |
| 1.5 | Rated capacity | 4200mAh (Rated discharge (0.2C) capacity after recommended charge.) |
| 1.6 | Minimum capacity | 4100mAh (Rated discharge (1C) capacity after recommended charge.) |
| 1.7 | Nominal voltage | 3.7V |
| 1.8 | Voltage of leave factory | 3.8V - 3.9V (Approximate state of charge = 50~80%) |
| 1.9 | Internal resistance of leave factory | <25mΩ (By resistance meter with AC 1 kHz.) |
| 1.10 | Maximum charge voltage | 4.2±0.05V(Acceptable maximum voltage) |
| 1.11 | Charging time | Rated charge：120min Reference 1a |
| 1.12 | Operating temperature | Charging：0～45°C Discharging：-20～60°C |
| 1.13 | Storage temperature | 1 year：-20～25°C 3 months：-30～45°C |
| 1.14 | Maximum continuous charging current | 6A(Acceptable maximal continuous charging current) |
| 1.15 | Dimension | (D)26.20*(H)66.40mm |
| 1.16 | Weight | 90.0±1.0g |

# 2. Pictures

# 3. Discharge Curve

# Text boxes

KEEPPOWER TECHNOLOGY CO., LIMITED

ADD: 5F, Bldg 4, Fenmenao Industrial Park, Bantian, Shenzhen 518129, China

TEL: +86 755 8995 6056         FAX: +86 755 8930 9659